Thermal Simulation Report and Model

MPC7448 High-Performance PowerPC Processor

July 4, 2005

Information in this report is property of Freescale Semiconductor, Inc.

Package Description:

MPC7448 package is 360 25x25 FC-HiCTE BGA or LGA, where:

- 360 is the number of spheres or pads on the device

- BGA means Ball Grid Array (spheres on 1.27 mm centers)

- LGA means Land Grid Array (no spheres - pads on 1.27 mm centers)

- 25mm x 25mm is the device body size

- FC-HiCTE means Flip-Chip with High Coefficient of Thermal Expansion ceramic substrate material

Case Outline Number: 98ARE10584D for LGA package

98ARE10538D for BGA package

Substrate Drawing: 18ARE10534D

Die Size: 8x7.3x0.86 mm

Table of Thermal Resistance Data

| Rating |  |  | Value | Unit | Notes |
| --- | --- | --- | --- | --- | --- |
| Junction to Ambient Natural Convection | Single Layer board (1s) | RJA | 26 | °C/W | 1,2 |
| Junction to Ambient Natural Convection | Four layer board (2s2p) | RJA | 19 | °C/W | 1,3 |
| Junction to Ambient (@200 ft/min) | Single layer board (1s) | RJMA | 22 | °C/W | 1,3 |
| Junction to Ambient (@200 ft/min) | Four layer board (2s2p) | RJMA | 16 | °C/W | 1,3 |
| Junction to Board |  | RJB | 11 | °C/W | 4 |
| Junction to Case |  | RJC | <0.1 | °C/W | 5 |

Notes:

1. Junction temperature is a function of die size, on-chip power dissipation, package thermal resistance, mounting site (board) temperature, ambient temperature, air flow, power dissipation of other components on the board, and board thermal resistance.

2. Per JEDEC JESD51-2 with the single layer board (JESD51-3) horizontal.

3. Per JEDEC JESD51-6 with the board (JESD51-7) horizontal.

4. Thermal resistance between the die and the printed circuit board per JEDEC JESD51-8.  Board temperature is measured on the top surface of the board near the package.

5. Thermal resistance between the active surface of the die and the case top surface determined by the cold plate method (MIL SPEC-883, Method 1012.1) with the calculated case temperature.  Actual thermal resistance is less than 0.1 °C/W.

6. Thermal characterization parameter indicating the temperature difference between package top and the junction temperature per JEDEC JESD51-2.  When Greek letters are not available, the thermal characterization parameter is written as Psi-JT.

The thermal performance of the LGA and the BGA versions of the package are the same.  For the thermal model, the only difference is the height of the package.

# Recommended Thermal Model, 360 25x25 mm FC-CBGA

For system thermal modeling, the MPC7448 thermal model is shown in Figure 1.  Four cuboids are used to represent this device.  The die is modeled as 8x7.3 mm at a thickness of 0.86 mm.  Contact Freescale Application Engineering for the appropriate power dissipation values.  The substrate is modeled as a single block 25x25x1.14 mm with orthotropic conductivity.   The die is centered on the substrate.  The bump/underfill layer is modeled as a collapsed resistance between the die and substrate assuming a conductivity of 5.0 W/m•K in the thickness dimension of 0.07 mm.  The C5 solder layer is modeled as a cuboid with dimensions 25x25x0.8 mm.

Table of geometry and conductivities for no Lid

| Conductivity | Value | Units |
| --- | --- | --- |
| Die (8x7.3x0.86mm) |  |  |
| Silicon | Temperature dependent |  |
| Bump/Underfill (8x7.3x.070mm) Collapsed resistance |  |  |
| Kz | 5.0 | W/m•K |
| Substrate (25x25x1.14 mm) |  |  |
| Kx | 9.9 | W/m•K |
| Ky | 9.9 |  |
| Kz | 2.95 |  |
| C5 solder layer (25x25x0.8mm) |  |  |
| Kx | 0.034 | W/m•K |
| Ky | 0.034 |  |
| Kz | 11.2 |  |

Figure 1.  Thermal Model for MPC7448.

Substrate

Bump/underfill

Die

C5 solder

Recommended Thermal model for LGA Package (360 25x25 FC-LGA)

The only difference between the FC-LGA and the FC-CBGA is that the thickness of the C5 solder layer is approximately 0.1 mm (depends on volume of solder paste used in circuit board assembly process) in the FC-LGA as opposed to 0.8 mm in the FC-CBGA.  All other package dimensions and material properties are the same.  The thermal performance is also the same, to within engineering tolerance.

The Flotherm library files of the parts have a dense grid to accurately resolve the laminar boundary layer for flow over the part in standard JEDEC environments, as well as the heat spreading in the board under the package.  In a real system, however, the part will require a heat sink to be mounted on it.  In this case, the predominant heat flow path will be from the die to the heat sink.  Grid density lower than currently in the package library file will suffice for these simulations.  The user will need to determine the optimal grid for their specific case.